**Comparison of Ni0.6Co0.4Fe2O4  and NiFe2O4 nanoparticles for magnetic characteristics, synthesized using co-precipitation method**

**Utari 1, Yeni Herlina K. Dasi 1,2, Budi Purnama1**

1Department of Physics, Graduate School, Sebelas Maret University Jalan Ir. Sutami 36 A, Surakarta 57126

2School of Engineering and Science, Institute Technology Dili, Rua ai -meti laran, Dili Timur Leste

E-mail: utarisby2013@staff.uns.ac.id

**Abstract:** Comparison of nickel Ni0.6Co0.4Fe2O4  and NiFe2O4were studied. The co-precipitation method was performed for the whole sample. After annealing of 600°C for 4 hours, the nanoparticles samples evaluated their structural properties by using Fourier Transform Infra-Red (FTIR) and X-Ray Diffraction (XRD). The XRD pattern confirms that the whole samples have the crystalline structure of the face-centered cubic (fcc) inverse spinel. Furthermore, the lattice and crystallite size of NiFe2O4 increased when added Co2+. The FTIR spectrum showed two prominent absorption bands, i.e., at around k of 358 cm-1 and 588 cm-1, where metals at tetrahedral and octahedral sites reflect intrinsic vibrations, respectively. Finally, the decrease of saturated magnetization *M*S from 22.2 emu/g and 9.92 emu/g replacement of Co2+ cation with Ni2+.

**Keywords:** Nickel, Co-precipitation, Crystallite, magnetic characteristic

1. **Introduction**

Due to technological interests and attractive magnetic properties, the synthesis of spinel ferrite nanoparticles is becoming one of the most popular research fields. One essential spinel ferrite is cobalt ferrite which exhibits relatively high curie, high magnetostrictive coefficient, and appropriate saturation magnetization and electrical insulation [1-3]. These promising properties of cobalt ferrite allow it to be applied in various fields of high-density digital recording devices [4], medical applications [5], catalysts [6], and others. In addition to its interesting application, changing the magnetic properties of cobalt ferrite can be done by adding doping to replace the ions in divalent or trivalent ions [7-8]. As in the research conducted by Kwang Joo Kim *et al.,* it was found that the Ni0.5Co0.5Fe2O4 thin films made by the sol-gel process have spinel structure with lattice parameters that were slightly smaller by 0.1% compared to CoFe2O4. Where Co ions occupy the tetrahedral and octahedral sites, while Ni ions occupy most of the octahedral sites of the spinel lattice. Saturation magnetization, remanent magnetization, and Coercive field of Ni0.5Co0.5Fe2O4 were reduced to 62%, 68%, and 29% [9].

Nickel ferrite (NiFe2O4) nanoparticles are ferrite spinel magnetic nanoparticles with properties such as low melting point, high specific heating, expansion coefficient is large, saturation magnetic moment low magnetic transition temperature [10-11]. NiFe2O4 nanoparticles are cubic ferromagnetic oxides with high permeability at high frequencies and high electrical resistance [12]. NiFe2O4 nanoparticles exhibit ferromagnetic properties due to the anti-parallel magnetic moment pairing between the magnetic moments of Fe3+ ions in the tetrahedral position. with the magnetic moments of Ni2+ ions and Fe3+ ions in the octahedral position. This ferrite system’s remarkable electrical and magnetic properties depend on the properties of the ions, and the distribution between the tetrahedral and octahedral positions. NiFe2O4 nanoparticles are soft ferrite material with characteristic ferromagnetic properties, low conductivity and low eddy current losses, high electrochemical stability, catalytic behavior and are widely available in nature [15]. NiFe2O4 and CoFe2O4 have an inverted spinel structure where (Ni2+Co2+) [Fe23+] O42- generally Fe3+ are in octahedral and tetrahedral sites while Ni2+ and Co2+ are in octahedral sites [16].

There are two categories of 'bottom-up' and 'top-down' spinel ferrite synthesis methods. During 'bottom-up,’ particles are formed when ions chemically combine. In the 'bottom-up, there are many synthesis techniques: the co-precipitation technique. Co-precipitation is widely used because it is cost and time-efficient, environmentally friendly, and has high mass production [17-18]. This research will discuss the comparison of Ni0.6Co0.4Fe2O4 and NiFe2O4. The NixCo1-xFe2O4 nanoparticle samples were synthesized using the co-precipitation method. Fourier transform infra-red (FTIR), x-ray diffractometer (XRD) were used to characterize the samples obtained, and magnetometry sample (VSM).

1. **Experimental**

**2.1. Material**

All the materials used in this report ware of analytical grade and used without further purification Ni (NO3)2, Co (NO3)2.6H2O, Fe (NO3)3.9H2O, and Sodium hydroxide.

**2.2. Synthesis of Ni0.6Co0.4Fe2O4 and NiFe2 O4**

The synthesis process is carried out through co-precipitation techniques, dissolving Ni (NO3)2, Co (NO3)2.6H2O, and Fe (NO3)3.9H2O for Ni0.6Co0.4Fe2O4 nanoparticles. Whereas NiFe2 O4 nanoparticles, made by dissolving Ni (NO3)2 and Fe (NO3)3.9H2O each with 200 ml of aqua-bides. Furthermore, it stirred using a *magnetic stirrer* at a speed of 300 rpm and heated at 3500C above the *hot-plan* until it reached a temperature of 950C. Then, the titration process is carried out by mixing 4.8 M Na OH into the solution (drop by drop). During the titration process, the solution temperature is maintained at 950C. The synthesis solution is deposited for one night, then washed six times using ethanol and distilled water. Then, the precipitate was dried using an oven for 12 hours with a controlled temperature of 1000C and crushed to fine by mortar. Samples of Ni0.6Co0.4Fe2O4and NiFe2 O4 were in a *furnace* with 6000C aneling temperature variations and then crushed again for homogeneous results.

* 1. **Characterizations studies**

The Ni0.6Co0.4Fe2O4 and NiFe2 O4 samples that had been formed were then characterized. The structural properties of samples were characterized using *Cu-Kα*, radiation = 1.54 Å) for X-Ray Diffraction (XRD) D8 Advance Diffractometer,

Bruker, USA. The *2θ* range was set at 25-70° with a step size of 0.02. The oxide bonds of the sample were characterized by Fourier Transforms Infrared (FTIR) spectroscopy (Shimadzu IR Prestige 21). The FTIR was recorded in the range 400- 4000 cm-1.

****

**Figure 1.** XRD pattern of NiFe2 O4 and Ni0.6 Co0.4 Fe2 O4 nanoparticles

1. Results and discussions

**3.1. X-ray diffraction studies**

X-ray diffraction pattern of NiFe2O4 and Ni0.6Co0.4Fe2O4 nanoparticles synthesized using the co-precipitation method at a temperature of 600 °C (figure 1). Diffraction pattern based on ICDD nickel ferrite and all the peaks matches the characteristic reflection. Different peaks appear in the XRD pattern, namely 2*θ* = 18.5°, 30.3°, 35.6°, 43.02°, 53.9°, 57.01°and 62.9°. Formation of an inverted spinel structure with sharp peaks and planes observed, indicating Fd3m space group symmetry with single-phase formation (JCPDS Card No. 1-1121) [18]. The calculation of the crystallite *D,* based on Scherrer’s equation

(1)

Where λ is the X-ray wavelength (1.540 Å), β is full width at half maximum (FWHM), and θ is the diffraction angle. Table 1 gives the increase in crystal size (D) in the presence of Cobalt ferrite, lattice parameter (a) of all samples calculated individually using the formula

 (2)

where d is the interplanar distance between two planes and (h, k, l) are the Miller indices. The lattice parameter value increased with the addition of cobalt ferrite from 8.85 to 13.81. This is caused by the fact that Co2+ has a larger ionic radius (0.74 ) than Ni2+ (0.69), having a smaller ionic radius, which causes unit cell contraction. The X-ray densities () was obtained from the equation

(3)

where M is the molecular weight of the sample, N is Avogadro’s number. The density of the sample with the addition of cobalt ferrite is smaller than that of nickel ferrite, and this is related to the crystal size of the sample. Lattermost, the nickel ferrite strains decreased from 8.85 to 13.817 with the addition of cobalt ferrite.

Table 1. The calculation of crystalline parameters of Ni0.6Co0.4Fe2O4 and NiFe2O4 nanoparticles

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sample | Crystallite size  *D* (nm) | Lattice parameter *a* (Å) | Density  *dx* (g/cm3) | Lattice strain  ε (x 10-3) |
| NiFe2 O4 | 8.85 | 8.352 | 5.344 | 12.80 |
| Ni0.2Co0.8Fe2O4 | 13.81 | 8.377 | 5.298 | 8.23 |

****

**Figure 2.** FTIR curves of NiFe2 O4 and Ni0.6 Co0.4 Fe2 O4 nanoparticles

**3.2. FTIR analysis**

FTIR characterization for the analysis of the oxide bond of Ni0.6Co0.4Fe2O4 and NiFe2O4 samples (Figure 1.2) with a range of 4000 cm-1 -350 cm-1. Characteristic of the observed curves for spinel ferrite, wave number v1 is in the range of 600 cm-1-500 cm-1 and wavenumber v2 is around 450 cm-1 -380 cm-1, which corresponds to the stretching of bonds between metal ions and oxygen at the tetrahedral and octahedral sites [19]. The absorption peaks observed for Ni0.6Co0.4Fe2O4 and NiFe2 O4 were around 588.3cm-1-558.42 cm-1 for the tetrahedral site and 376.14 cm-1 – 358.78 cm-1 for the octahedral site.

****

Figure 3. Hysteresis loop of NiFe2 O4 and Ni0.6Co0.4Fe2O4 nanoparticles synthesized

* 1. **VSM analysis**

The comparison of hysteresis loops between sample Ni0.6Co0.4Fe2O4 and NiFe2O4 has the same typical width and different saturation points (figure 3). Sample Ni0.6Co0.4Fe2O4 has a larger hysteresis than NiFe2O4. Table 3 shows the presence of the enhancement in Ms, Hc, and Mr, of Ni0.6Co0.4Fe2O4,compared to NiFe2O4. The presence of cobalt ion increased the Mr and Ms of nickel ferrite from 1.96 emu/g to 12.33 emu/g and 9.92 emu/g to 22.2 emu/g.

Table 2. Coercive field (*Hc)* and magnetization *(M*S*)* NiFe2O4 andNi0.6 Co0.4 Fe2O4 nanoparticles

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sample | *Hc (Oe)* | *M*S(emu/g) | *Mr*(emu/g) | *Mr/Ms* |
| NiFe**2**O4 | 123 | 9.92 | 1.96 | 0.379 |
| Ni0.6Co0.4Fe2O4 | 793 | 22.2 | 12.33 | 0.511 |

1. **Conclusion**

The suitable method obtained structural properties of NiFe2O4andNi0.6 Co0.4 Fe2 O4nanoparticles with an annealing temperature of 600oCfor 4 hours. The XRD diffraction pattern of the two samples based on nickel ferrite ICDD, an inverted spinel structure with sharp peaks and planes, was observed, showing the symmetry of the Fd3m space group. Then, the crystal size and lattice parameters in nickel ferrite increase with the addition of cobalt ferrite because Co2+ has a larger ionic radius than Ni2+, which has a smaller ionic radius. The FTIR spectrum showed two prominent absorption bands, namely around 588.3cm-1-558.42 cm -1 for the tetrahedral site and 376.14 cm-1 -358.78 cm-1 for the octahedral site. The presence of cobalt ions in octahedral sites increases the *Mr* and *M*S of nickel ferrite because the magnetic moment of cobalt is much greater than that of nickel.

**Acknowledgments**

This research was funded by DIPA PNBP Universitas Sebelas Maret, Kementerian Riset, Teknologi, dan Pendidikan Tinggi, The Republic of Indonesia, contract No. 516/UN27.21/PP/2020.

**References**

[1] M. Sedlacik, V. Pavlinek, P. Peer, P. Filip, Tailoring the magnetic properties and magnetorheological behavior of spinel nanocrystalline cobalt ferrit by varying annealing temperature, Dalton Trans. 43 (18) (2014) 6919–6924.

[2] F.E. Carvalho, L.V. Lemos, A.C.C. Migliano, J.P.B. Machado, R.C. Pullar, Structural and complex electromagnetic properties of cobalt ferrite (CoFe2O4) with an addition of niobium pentoxide, Ceram. Int. 44 (2018) 915–921, [https://doi.org/10. 1016/j.ceramint.2017.10.023](https://doi.org/10.%201016/j.ceramint.2017.10.023)

[3] Lima, A.C., Peres, A.P.S., Araujo, J.H., Morales, M.A., Medeiros, S.N., Soares, J.M., Melo, D.M.A., & Carrico, A.S. (2015). The effect of Sr2+ on the structure and magnetic properties of nanocrystalline cobalt ferrite.

[4] K.L. Routray, B. Sahoo, D. Behera, Structural, dielectric and magnetic properties of nano sized CoFe 2 O 4 employing various synthesis techniques for high frequency and magneto recording devices: a comparative analysis, Mater. Res. Express. 5 (2018) 085016, ,https://doi.org/10.1088/2053-1591/aad310

[5] S.Y. Srinivasan, K.M. Paknikar, D. Bodas, V. Gajbhiye, Applications of cobalt ferrite nanoparticles in biomedical nanotechnology, Nanomedicine 13 (2018) 1221–1238, <https://doi.org/10.2217/nnm-2017-0379>.

[6]A. Al-Anazi, W.H. Abdelraheem, C. Han, M.N. Nadagouda, L. Sygellou, M.K. Arfanis, P. Falaras, V.K. Sharma, D.D. Dionysiou, Cobalt ferrite nanoparticles with controlled composition-peroxymonosulfate mediated degradation of 2-phenylbenzimidazole-5 sulfonic acid, Appl. Catal. B Environ. 221 (2018) 266–279, <https://doi.org/10.1016/j.apcatb.2017.08.054>

[7]S. Anjum, F. Sehar, F. Bashir, M. S. Awan, and Z. Mustafa, vol. 2, no. 10. Elsevier Ltd., 2015.

[8]A. C. Lima *et al.*, *Mater. Lett.*, vol. 145, pp. 56–58, 2015, doi: 10.1016/j.matlet.2015.01.066.

[9] kwang Joo Kim,Jonggho Park, and Jae Yun Park, Cystallograpic and Magnetic Characreristics if Thim-film Ni0.5Co0.5Fe2O4Ferrimagnet, Journal of Magnetics 25(2),117-120 (2020)., <https://doi.org/10.4283/JMAG.2020.25.2.117>

[10]M. Parishani, A.Cheragi, R. Malekfar. “Spectroscopy, Structural and Optical Investigations of NiFe2O4 Ferrite”. InternationalJournal of Optics and Photonics (IJOP)”. vol. 9, no. 2, pp. 73-78, 2015.

[11]R. B. Bhise, S. M. Rathod, and A. K. Supekar. “Synthesis and Characterization of nanocrystalline Ni-Co-Zn ferrite by Sol-gel Auto-Combustion Method”. International Journal of Scientific &Engineering Research , vol. 3, no. 12, pp. 1-5, Dec. 2012

[12] M. Penchal Reddy, W. Madhuri, K. Sadhana, I. G. Kim, K. N. Hui, K. S. Hui, K. V. Siva Kumar, and R. Ramakrishna Reddy. “Microwave sintering of Nickel Ferrite Nanoparticles Processed Via Sol-GelMethod”. J. Sol-Gel Sci. Technol., vol. 70, no. 3, pp. 400-404, June 2014

[13] P. Sivakumar, R. Ramesh, A. Ramanand, S. Ponnusamy and C. Muthamizhchelvan. “Synthesis and Characterization of NiFe2O4 Nanosheet Via Polymer Assisted Co-Precipitation Method, Materials Letters”. vol. 65, no. 3, pp. 483-485, Feb. 2011.

[14] K.K. Kefeni, T.A. Msagati, B.B. Mamba, Ferrite nanoparticles: synthesis, characterisation and applications in electronic device, Mater. Sci. Eng., B 215 (2017) 37–55.

[15] I. Safarik, K. Horska, K. Pospiskova, Z. Maderova, M. Safarikova, Microwave assisted synthesis of magnetically responsive composite materials, IEEE Trans. Magn. 49 (2012) 213–218.

[16] Lu LeT, Dung NgoT, Tung LeD, Thanh CT, Quy OK, Chuc NV, Maenosono S, Thanh NTK (2015) Synthesis of magnetic cobalt ferrite nanoparticles with controlled morphology, monodispersity and composition: the influence of solvent, surfactant, reductant and synthetic conditions. Nanoscale 7:19596–19610

[17] Qasim M, Asghar K, Singh BR, Prathapani S, Khan W, Naqvi AH, Das D (2015) Magnetically recyclable Ni0.5Zn0.5Fe2O4/ Zn0.95Ni0.05O4 nano-photocatalyst: structural, optical, magnetic and photocatalytic properties. Spectrochim Acta A: Molecul Biomolecul Spect 137:1348–1356

[18] Stein CR, Bezerra MTS, Holanda GHA, Andre-Filho J, Morais PC (2018) Structural and magnetic properties of cobalt ferrite nanoparticles synthesized by co-precipitation at increasing temperatures. AIP Adv 8:056303