BIOFILM CHITOSAN AS MODERN DRESSING FOR ULCERS

Romanna Cintya Madeleine Simanjuntak1, Wisye Riyoly1, Fiane de Fretes1, Agung Rimayanto Gintu2

1Nursing, Faculty of Medicine and Health Sciences Satya Wacana Christian University

Jl. Kartini No. 11A Salatiga Street, Central Java 50711, Indonesia

2Magister Biology, Faculty of Biology, Satya Wacana Christian University

Jl. Diponegoro No. 56-60 Salatiga Street, Central Java 50711, Indonesia

Correspondence: Phone: 089677965935, email: 462018018@student.uksw.edu

ABSTRAK

Modern dressing techniques as open wound dressings are still effective and suitable for use, especially for people with open wounds such as ulcers, but they still has disadvantages, such as the expensive prices and needs for other antibiotics to prevent inflammation. Previous studies reported an increase in the number of antibiotic resistance, which sparked the idea of producing new dressing materials that have strong antimicrobial and biocompatible properties. The material suitable for the idea of a wound dressing is chitosan biofilm because it has strong antibacterial properties and has a similar structure to the skin tissue. This study aims to produce chitosan biofilm using the deacetylation method using a strong base.The physicochemical characterization results of biofilms showed a deacetylation degree of 87.13 with a voltage of 1.15 ± 0.00 and a polycationic group of biofilms that appeared at a wave number of 2.1714 ± 0.0000 nm. From the measurement of the antibacterial power of chitosan biofilm against skin surface bacteria, the inhibition zone diameter was 18.93 ± 0.12; 19.50 ± 0.17; 20.20 ± 0.23; 20.13 ± 0.03 and 22.53 ± 0.09 against S. aureus, S. epidermidis, P. aeruginosa, E. colli, Bacillus sp. Overall, it can be concluded that biofilm chitosan has the opportunity to be applied as a dressing in wound care.

Key words: Antibacterial, Biofilm, Chitosan, Ulcers

Introduction

A wound is a broken off of tissue continuity or damage to the structure and anatomy of the skin due to injury or surgery (Kartika, 2015). One example of a wound that requires wound care with that proper technique is an ulcuscle. Diabetic ulcuscle often occur in the lower limb are at risk of causing amputation. (Agustin et al. 2015). Ulcuscle are open wounds on the skin surface, mucous membrane, mortality of extensive tissues and accompanied by invasive saprophytic bacteria  (Andyagreeni. 2010).

Diabetic Ulcers is usually experienced by patients with prolonged bed rest such as stroke patients. Ulcers occur on areas of the skin that

have been subject to prolonged pressure such as the back, calf or heel. Decubitus ulcers are at risk of causing infection to sepsis. (Setyawati et al.2015).

The principle of ulcers treatment is to maintain moisture and barrier of the tissues. The Moisture  of skin could support  the wound recovery (Merdekawati & AZ 2017). At the present, wound care has developed rapidly with advances in technology that support wound care recovery. The use many bandages or as a known dressing model has been available in Indonesia (Wijaya,2018). One example of bandage used at the present is modern dressing. According to the previous  study (Tiara  et al.2013) present that modern dressing techniques are effectively used for dressings or known as dressing models are available in Indonesia (Wijaya, 2018). The interventions given to ulcers are bandages or stockings (multi-layered, high compression) on identified complex wounds and wound cleaning for venous leg ulcers; four-layer bandages for mixed arterial/venous leg ulcers; biological dressings, ultrasounds, and hydrogels for diabetic foot or foot ulcers; hydrocolloid dressings, electrotherapy, air-water beds, and foam mattresses are alternatives to pressure Ulcers and silver bandage and ultrasound for unspecified mixed complex wounds (Tricco  et  al. 2015). According to the research (Tiara et al, 2013) present that modern dressing techniques are effectively used for wound recovery in diabetics compared to conventional techniques which take relatively longer time. However,  modern dressings also have weaknesses such as the price of treatment is quite expensive, the tools and materials can only be found in certain pharmacies and can only be done by nurses who have certificates (Endang & Kelvin, 2019).

Many nurses prefer to use antibiotics as another alternative for the treatment of diabetic mellitus ulcuscle wounds. The usual topical antibiotic is erythromycin. However, the previous study (Patil, et al2018) showed that antibiotics erythromycin, tetracycline and ciprofloxacin have high rates of antibiotic resistance. The conventional drugs don't show  a significant effect for tissue improvement, but the cause of wound due to the effects of the administration of antibiotics that are not appropriate or do not correspond to the type of bacteria.

In the research data on the effectiveness of antibiotics in diabetic patients showed that the antibiotics on the foot ulcuscle of DM patients was about 78.94% effective and 21.05% ineffective due to bacteria resistant to all types of antibiotics given (Angistia, et al. 2017). This research is analogous with research conducted by Hatanta 2013, regarding the study of antibiotic use in showing that some bacteria experience resistance to antibiotics given empirically, such as the types of bacteria: cefotaxime, ceftriaxon, and ciprofloxacin.

The increase in antibiotic retention rate has led to an increase in the use of natural  ingredients that contain antimicrobial compounds such as chitosan, because the bioactive compounds can inhibit the growth of bacteria by damaging the cell membrane of bacteries bacteria (Damayanti et al. 2016). Chitosan is a natural compound build the crustacean shells shells that contain active metabolites that are antibacterial or have activity against E.Coli, Vibrio Cholerae, Shigella dysenteriae  and  Bacteroides fragilis  (Rahmayanti et al. 2018). According to Putri & Tasminatun (2012) states that chitosan is a natural biopolymer derived from chitin, the main component of external crustaceans  such as shrimp and crab shells. Some studies have shown that chitosan is effective in accelerating wound recovery because it has specific properties that are bioactive, biocompatible, anti-bacterial, anti-fungal  and biodegradable. Chitosan has long been used for bacteriostatic, immunology, anti-tumor,  cicatrizant,  homeostatic and anticoagulant, ointments for wounds, eye medicine, orthopedics, and surgical suture recovery (Pratiwi, 2014). In addition, Chitosan can also be applied to tooth extraction  scars before closing the wound (Gunawan,  et al.2015). In Indonesia, generally the material used as a source of Chitosan is waste shrimp shells, but it has not been fully utilized so that it can be obtained at a low price and even for free. Based on the opportunity of shrimp shell waste in Indonesia and its easy application. The aim of this study was to produce chitosan biofilms that can be applied to the surface of the wound skin. The use of biofilms as wound covers provides several benefits such as repairing damaged skin tissue,  stopping bleeding and preventing infection. Chitosan biofilms that are already available can be marketed to the medical world such as Hospitals, Health Centers, Pharmacies and even cosmetic industry companies. Chitosan biofilms can solve the problem of people's needs for   antibiotic materials that are low toxicity, minimum side effect, biocompatible, biodegradable  and can be a repair agent damaged skin tissue.

Method

Nano chitosan biofilm research was conducted at the Universitas Kristen Satya Wacana (UKSW) FKIK Lab, in collaboration with related fields of science. Samples in the form of tiger shrimp shells (Panaeus Monodon) can be obtained from Pasar Raya Salatiga, Salatiga City, Central of Java or fish-based food processing businesses around the city of Salatiga. The tools used in this study were a knife, spatula, magnetic stirrer, acid bath, thermometer, viscometer and UV-VIS spectrophotometer. The chemicals used are hydrochloric acid (HCl), acetic acid (vinegar), NaOH, and NaPO4, all of which are in the Pro-Analysis (PA) category.

- Synthesis of Chitin from Shrimp Shells

Shrimp shells obtained from the market are washed with H2O2 and dried for 3 hours using the oven at 80oC. After drying, shrimp shells are moderated  in 500 mL of HCl 5% (v/v) for 24 hours to remove minerals. After 24 hours, the shrimp shells are washed to a neutral pH and dried. After drying, maceration of shrimp shells continued using  500 mL of NaOH 4% (w/v) for 24 hours to remove protein and fat from shrimp shells. After 24 hours, a pure white chitin polymer sheet was obtained, chitin was then rinsed to neutral pH and then dried (Islam  et al. 2011; Rochima, 2007).

- Synthesis of Chitosan from Chitin

Chitin obtained from the shrimp shells was macerated in 70% (w / v) NaOH solution with a ratio of 1g of sample in 25 mL of 70% NaOH. Maceration is carried out at a temperature of 120-130oC for 90 minutes to eliminate acetamin groups from chitin. After 90 minutes, a yellowish white polymer chitosan was obtained. Chitosan is washed and rinsed to neutral pH then dried, to qualitatively test the formation of chitosan, 0.5g of chitosan is taken and then dissolved in 5 mL of 1-5% (v / v) acetic acid if a gel is formed, it means that the polymer obtained is chitosan and deacetylation is successful (Islam et al, 2011; Rochima, 2007).

- Synthesis of Nano Chitosan

Take 10 ml of 1% chitosan solution and then drop it with 10% phosphoric acid to form a fine white precipitate, the precipitate is then separated from the solution and dried (Kurniasih and Dwi, 2011; Mardliyanti et al. 2012; Komariah, 2015).

- Chitosan Biofilm Making

Taken 10 ml of Chitosan gel and poured into a mold container measuring 5 x 2 cm2 and mold container then flattened and dried at room temperature. After drying, the biofilm can be removed from the mold. For large scale needs, chitosan gel can be poured on a large glass plate and then dried and cut to the size needed.

- Use in Wound Handling

mold container then flattened and dried at room temperature. After drying, the biofilm can be removed from the mold. For large scale needs, chitosan gel can be poured on a large glass plate and then dried and cut to the size needed.

Results and Discussions

Shrimp shells were chosen as chitosan synthesis material because the abundance of shrimp shells in Indonesia is very large and can be obtained at a relatively cheap price. In shrimp shells, natural biocontrol of the active ingredient chitin / chitosan was found (Marni & Maria, 2016). Shrimp production capacity in Indonesia reaches 500,000 tons per year by producing around 300,000 tons of waste from 170 units of shrimp processing industry (Sismaraini, 2015). This waste is used as material to produce synthetic chitosan. The production of nano chitosan biofilm was carried out at the FKIK UKSW Lab, in collaboration with related fields of science. The results of the shrimp shell characterization are shown in Table 1.

Table 1. GraphmetricAlly Measured Mineral Content in Shrimp Shells

| Parameter | Ingredients InX ( ± SE): |  |  |  |
| --- | --- | --- | --- | --- |
|  | Shrimp Shells | Chitin | Chitosan | Chitosan TPP |
| Water (%) | 0,1167 ± 0,0082 | 0,10 ± 0,00 | 0,10 ± 0,00 | - |
| Both (g/g) | 0,0071 ± 0,0003 | 0,0059 ± 0,0002 | 0,0057 ± 0,0001 | - |
| SiO (g/g) | 0,0023 ± 0,0001 | 0,0014 ± 0,0002 | 0,0013 ± 0,0001 | - |
| Organic Matter (g/g) | 0,9929 ± 0,0003 | 0,9941 ± 0,0002 | 0,9943 ± 0,0001 | - |
| Organic Carbon (g/g) | 0,5759 ± 0,0002 | 0,5766 ± 0,0001 | 0,5767 ± 0,0001 | - |
| N Total (%) | 11,05 ± 0,0120 | 2,72 ± 0,0797 | 0,25 ± 0,0203 | - |
| Fat (%) | 5,31 ± 0,1747 | 2,20 ± 0,1000 | 0,06 ± 0,0067 | - |
| PO4 (g/g) | 0,0942 ± 0,0023 | 0,0870 ± 0,0006 | 0,0205 ± 0,0002 | 0,0896 ± 0,0001 |
| P2O5 Available (g/g) | 0,0052 ± 0,0002 | 0,0049 ± 0,0001 | 0,0035 ± 0,0002 | 0,0055 ± 0,0003 |
| Dissolved P2O5 (g/g) | 0,0025 ± 0,0001 | 0,0022 ± 0,0001 | 0,0017 ± 0,0001 | 0,0022 ± 0,0001 |
| P2O5 Total (g/g) | 0,0071 ± 0,0002 | 0,0075 ± 0,0001 | 0,0043 ± 0,0001 | 0,0076 ± 0,0001 |
| Total P (g/g) | 0,0593 ± 0,0020 | 0,0219 ± 0,0002 | 0,0054 ± 0,0002 | 0,0421 ± 0,0005 |
| Deasetilasi (%) | - | 18,05 | 87,13 | 66,22 |
| Rendemen (%) | - | 10,52 ± 0,0233 | 79,59 ± 0,0504 | 0,54 ± 0,0203 |

The N content of 11.05 ± 0.0120 in shrimp shells indicates that shrimp shells can be used as a source of synthetic chitosan which has a great opportunity in its application. The synthetic yield of shrimp shells also showed a fairly large chance of success, namely 79.59 ± 0.0504. Furthermore, physicochemical characterization of synthetic chitosan from shrimp shells was carried out to determine the chemical properties of chitosan as the first step in applying chitosan as an antibacterial active ingredient. The results of chitosan characterization are shown in Table 2.

Table 2. Characteristics of Chitosan and Chitosan Treatment Results

| Products | Brix (%) | Density (g/cc) | Viscositas |  |  | W (g/mol) | Keelektrikan |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Absolute (P.a) | Kinetics (Cts) | Dynamic (CPs) |  | Voltage (mV) | Current Strength (mA) | Electrical Resistance (Ohm) |
| Chitosan Gel | 5,1 ± 0,00 | 1,1251 ± 0,0005 | 2,10 ± 0,0000 | 1,87 ± 0,0009 | 4,76 ± 0,0000 | 2,1714 ± 0,0000 | 1,15 ± 0,00 | 20 ± 0,00 | 62 ± 0,00 |
| Chitosan 1% | 10,13 ± 0,03 | 0,8808 ± 0,0112 | 1,10 ± 0,0577 | 1,25 ± 0,0790 | 9,14 ± 0,4818 | 1,1374 ± 0,0597 | 1,20 ± 0,00 | 50 ± 0,00 | 54 ± 0,00 |
| Chitosan TPP | 1,2 ± 0,00 | 0,9967 ± 0m0036 | 1,50 ± 0,0000 | 1,51 ± 0,0055 | 6,67 ± 0,0000 | 1,5510 ± 0,0000 | 2,70 ± 0,00 | 35 ± 0,00 | 54 ± 0,00 |

Based on the results of the characteristics of chitosan, it is known that TPP chitosan has adhesiveness, flexibility and antibacterial power that is stronger than that of chitosan gel and 1% chitosan. Giving chitosan to wounds greatly affects the healing process, with the initial stage marked by inflammation causing tissue and blood vessel damage, resulting in platelets (platelets) coming out and forming blood clots (blood clots) which can accelerate the healing process in wounds (Prastika et al. 2020). The results of this study are supported by the results of previous studies (Ueno et al. 2001) which state that giving chitosan can trigger macrophage cells to increase the production of growth factors such as PDGF, FGF and TGFβ so that they can accelerate the process of fibroblasts in proliferation, migration and forming an extracellular matrix. The increasing number of fibroblast cells, the more collagen produced will also increase. So that the process of synthesis and collagen degradation can be balanced (Prastika et al. 2020). In Wadaniati and Sugiyanti's research (2009) states that chitosan has great potential to be used as an antibacterial agent, because it contains lysozyme enzymes and aminopolysacharida groups which can inhibit bacterial growth by inhibiting chitosan in bacteria. The results of research obtained by (Suherman et al. 2018) stated that shrimp shells chitosan is effective as an antibacterial which can inhibit the growth of the bacteria Staphylococcus Epidermidis Pseudomonas Eruginosa, Propionibacterium Agnes, including E. Coli.

Chitosan is Osteoconductive, bioactive which can improve the wound recovery process, so Chitosan has been widely used in the medical field because it has antimicrobial properties that make it attractive to use as a bioactive coating. Chitosan also allows for tissue growth when combined with calcium phosphate compounds (Zhao et al. 2002).

Table 3. Antibacterial Power of Chitosan and Chitosan TPP (Nano) Based on  Average Diameter of Inhibitory Zone (DIZ)

|  | Diameter of Bland Area (DIZ) (mm) Against Bacteria |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | S. aureus | S. epidermidis | P. aeruginosa | E. colli | Bacillus sp |
| Chitosan Gel | 18.93 ± 0,12 | 19,50 ± 0,17 | 20,20 ± 0,23 | 20,13 ± 0,03 | 22,53 ± 0,09 |
| Kitosan TPP | 17,23 ± 0,19 | 20,47 ± 0,08 | 16,40 ± 0,26 | 20,43 ± 0,12 | 21,53 ± 0,19 |
| Tetracycline | 21,23 ± 0,15 | 21,00 ± 0,00 | 23,93 ± 0,15 | 22,67 ± 0,19 | 25,67 ± 0,19 |
| Streptomycin | 21,47 ± 0,12 | 21,13 ± 0,03 | 20,87 ± 0,03 | 21,07 ± 0,19 | 21,87 ± 0,03 |
| Erythromycin | 22,77 ± 0,07 | 22,80 ± 0,06 | 23,30 ± 0,10 | 25,90 ± 0,17 | 26,60 ± 0,10 |

The table above proves that chitosan has strong antibacterial resistance against bacteria on the skin surface. Antibacterials are needed on wounds to get rid of bacteria because they can cause infection. The bacteria that most often produce pus (pus) are Staphylococcus aureus, Klebsiella spp (Kumar, 2013). The results of research by Yunianto et al. 2017 showed that the ointment with the active ingredient Curcuma aeruginosa has a diameter (14.52 mm), C.longa L (13.26 mm) and C.xhantoriza L (7.89 mm). This proves that the inhibitory power of chitosan is much greater than the active ingredients of kencur, turmeric and temugiring.

Figure 1. In vitro Biofilm					Figure 2. In vitro Biofilm

Wadaniati and Sugiyanti (2009)		 		    Islam  et al  (2011)

The characterization results in the in vitro biofilm image above show that there is a tug-of-war interaction between the polycationic group of chitosan and phospholipids in the skin tissue to produce protein fiber joints that cover the wound.

Biofilm Chitosan Images

(Author Documentation)

The chitosan biofilm image above shows that chitosan gel can be used as a biofilm which has a great opportunity as a wound cover in ulcers with antibacterial resistance. Biofilms are designed to be applied to wounds using a bandage. In addition, the resulting biofilm has a clear and transparent color so it is different from other biofilms. Wounds that have been covered by biofilm do not need to be cleaned repeatedly, because their clear and transparent color makes it easier to see the wound healing process or an infection in the wound. So that this biofilm can be a new innovation that can be used in the medical world for handling ulciscle in wounds.

Conclusion

Diabetic ulcers is one of the wounds that requires special care appropriately and correctly. The use of antibiotics in wound management is still high and has insignificant effects. One of the natural ingredients that can be used as an opportunity in handling diabetic ulcers is chitosan. Chitosan is one of the ingredients found in outer crustaceans such as shrimp, crab and shellfish shells. The cleaned shrimp shells are synthesized to produce chitosan and processed into gel into biofilm. The results of the Inhibited Area Diameter (DDH) against Skin Surface Bacteria showed is chitosan. Citosan had a strong antibacterial resistance. Based on the results the characteristic in vitro of chitosan biofilm, has an interesting interaction between polycationic groups of chitosan and phospholipids on the skin tissue. Chitosan also helps increase the number of macrophage cells to speed up wound recovery. The result of biofilm can be a new innovation for the medical industry because it is clear, transparent and easy to apply to the ulcers.

Reference

Adam Syamsunir. 1992. “Dasar-Dasar Mikrobiologi dan Parasitologi untuk Perawat” :Jakarta. Buku Kedokteran EGC

Agistia Nesa, Muchtar Husri, Nasif Hansen. “Efektivitas Antibiotik Pada Pasien Ulkus Kaki Diabetik”. Jurnal Sains Farmasi dan Klinis. 2017;4(2):43-48.

Agustin Rima Wahyu, Safitri Wahyuningsi, Oktovianus. 2015. “Pengaruh Microfiber Triangle Pillow Terhadap Kejadian Ulkus Dekubitus Pada Immobilisasi Di Ruang Perawatan”. Jurnal KesMaDaSka - Januari 2015.

Agustini, T.W. & Sedjati, S., 2006. The Effect of Chitosan Concentration and Storage Time on the Quality of Salted – Dried Anchovy (Stolephorus heterolobus).

Andrea C Tricco, Jesmin Antony, Afshin Vafaei Paul A Khan, Alana Harrington, Elise Cogo, Charlotte Wilson, Laure Perrier, Wing Hui dan Sharon E Straus. 2015 “ Seeking effective interventions to treat complex wounds: an overview of systematic reviews” Tricco et al. BMC Medicine (2015) 13:89 DOI 10.1186/s12916-015-0288-5.

Andyagreeni. (2010). Tanda Klinis Penyakit Diabetes Mellitus. Jakarta: CV.Trans Info Media.

Damayanti Windi, Rochima Emma, Hasan Zahida. 2016 “Aplikasi Kitosan Sebagai Antibakteri Pada Filet Patin Selama Penyimpanan Suhu Rendah” 2016, Volume 19 Nomor 3. Available online: journal.ipb.ac.id/index.php/jphpi

Dawley Rats Perbandingan Tingkat Kesembuhan Luka Bakar Derajat II Antara Pemberian Madu Dengan Tumbukan Daun Binahong Pada Tikus. Journal Majority.Vol.6 No.1, 2015:103–12.

Endang Subandi & Kelvin Adam Sanjaya. 2019. “Efektivitas Modern Dressing Terhadap Proses Penyembuhan Luka Diabetes Melitus Tipe 2”. Jurnal Kesehatan, Vol. 10 No. 1 Tahun 2019

gelation network composite scaffolds. Biomaterials 23:3227-3234.

Gunawan Felinda, Sularsih, Soemartono. 2015 “Perbedaan Kitosan Berat Molekul Rendah dan Tinggi Terhadap Jumlah Sel Limfosit Pada Proses Penyembuhan Luka Pencabut Gigi”. Vol. 9 No. 1 Februari 2015. ISSN: 1907-5987

Hatanta, A. “Kajian Penggunaan Antibiotik Pada Pasien Infeksi Ulkus Kaki Diabetik IRNA Penyakit Dalam RSUP Dr. M. Djamil Padang”. (Tesis). Universitas Andalas. Padang; 2013.

Hui Liu, Yumin Du, Xiaohui Wang, Liping Sun, 2004. Chitosan Kills Bacteria through Cell Membrane Damage. International Journal of Food Microbiology. 95:147– 155.

Kartika W. Ronald. 2015. “Perawatan Luka Kronis dengan Modern Dressing” Bagian Bedah Jantung Paru dan Pembuluh Darah Wound Care/Diabetic Center, RS Gading Pluit, Jakarta: CDK-230/ vol. 42 no. 7, th. 2015

Kumar A.R. 2013. Antimicrobial Sensitivity Pattern of Klebsiella pneumonia Isolated from Pus from Tertiarycare Hospital and Issue Related to the Rational Selection of Antimicrobials. Journal of chemical and Pharmaceutical Research. 5(11): 326-331.

Marni Kaimudin & Maria F Leounupun. 2016. “Karakteristik Kitosan dari Limbah Udang dengan Prose Bleaching dan Deasetilasi yang Berbeda” Received : 10/02/2016 ; Revised : 26/02/2016 ; Accepted : 27/04/2016 ; Published online : 30/06/2016

Maryunani, Anik. 2013. “Perawatan Luka (Modern Wound Care) Terlengkap dan Terkini" Jakarta : In Media

Menteri Kesehatan RI. 2011. Peraturan Menteri Kesehatan Republik Indonesia Nomor 2406/Menkes/Per/XII/2011 Tentang Pedoman Umum Penggunaan Antibiotik

Merdekawati Diah & AZ Rasyidah, 2017. “Hubungan Prinsip dan Jenis Balutan dengan penerapan Teknik Moist Wound Healing”

Prasetya Fajar. 2011. “Evaluasi Penggunaan Antibiotika Berdasarkan Kontraindikasi, Efek Samping, Dan Interaksi Obat Pada Pasien Rawat Inap Dengan Infeksi Saluran Pernapasan Bawah Di Rumah Sakit Panti Rapih Yogyakarta Periode Januari-Juni 2005” J. Trop. Pharm.  Chem. 2011. Vol 1. No. 2

Prastika Dwi Dinda, Setiawan Boedi, Saputro Logam Amung, Ida Sari Yudaniayanti, Wibawati Ayu Prima dan Fikri Faisal. 2020. “Pengaruh Kitosan Udang Secara Topikal Terhadap Kepadatan Kolagen Dalam Penyembuhan Luka Eksisi Pada Tikus Putih”. J Med Vet 2020, 3(1):101-107. pISSN: 2615-7497; eISSN: 2581-012X | 10.

Pratiwi R. “Manfaat kitin dan kitosan bagi kehidupan manusia”. Oseana. 2014; 39(1):35-43.

Putri FR, Tasminatun S. “Efektivitas Salep Kitosan terhadap Penyembuhan Luka Bakar Kimia pada Rattus norvegicus”. Mutiara Medika. 2012; 12(1):24-30.9.

Rahmayanti Sari, Khotima Siti, Pramanayudha Gilang. 2018. “Uji Aktivitas Antibakteri Senyawa Kitosan terhadap Neisseria gonorrhoeae yang diisolasi dari Pasien dengan Penyakit Infeksi Seksual secara In Vitro”. Jurnal Cerebellum. Volume 4. Nomor 3. Agustus 2018.

Rusnoto, Chandiq, N., & Winarto. 2017. “Pengetahuan dan Kepatuhan Kontrol Gula Darah Sebagai Pencegahan Ulkus Diabetikum. The 6th University Research Colloquium 2017 Universitas Muhammadiyah Malang”

Setyawati Reno, Suyanto, Noor Arifin Mohammad. 2015. Pengaruh Mobilitas dan Penggunaan VCO (Virgin Coconut Oil) Terhadap Ulkus Dekubitus Pada Gangguan Fungsi Motorik Pasca Stroke. Nurscope. Jurnal Keperawatan dan Pemikiran Ilmiah. 1 (1). 1-7

Sismaraini D. (2015) “Strategi Pengembangan Industri Kitin Dan Kitosan Di Indonesia. Tesis. Sekolah Pascasarjana Program Studi Teknologi Industri Pertanian. Bogor” : Institut Pertanian Bogor.

Suherman B, Latif Muhdar & Dewi Rosmala Teresia Sisilia. 2018 “Potensi Kulit Udang Vannamei (Litopenaeus Vannamei) Sebagai Antibakteri Terhadap Staphylococcus Epidermidis, Pseudomonas Aeruginosa, Propionibacterium Agnes, dan Escherichia Coli Dengan Metode Difusi Cakram Kertas”. Media Farmasi Vol. XIV. No. 1. April 2018

Suptijah Pipih, Jacob M Agoes, Mursid Sugara. 2010. “Teknik Peranan Kitosan Dalam Peningkatan Pertumbuhan Tomat (Lycopersicum Esculentum) Selama Fase Vegetatif”. Akuatik-jurnal sumberdaya perairan Volume 4 no. 1 tahun 2010.

Syuhar MN , Windarti I, Kurniawati E. The Comparison of Second Degree Burns Healing Rate Between The Smear of Honey And The Collision of Binahong Leaves In Sprague

Tharik Ath Reizal M, Rahmat Anisa, Fadli Ahmad & Handayani Rani. “Pengembangan Kitosan Terkini Pada Berbagai Aplikasi Kehidupan:review”.

Tiara, S., N. I. W. Sukawana, S. Kep, dkk. 2013. “Efektivitas Perawatan Luka Kaki Diabetik Menggunakan Balutan Modern Di RSUP Sanglah Denpasar dan Klinik Dahlia Care”. Program Studi Ilmu Keperawatan Fakultas Kedokteran Universitas Udayana 1(1) :6.261

Utami rahayu Eka. 2012. “Antibiotika, Resistensi dan Rasionalitas Terapi”. Sainstis. Volume 1, Nomor 1, April – September 2012. Issn: 2089-0699.

Wijaya Sukma Made, 2018. “Perawatan Luka dengan Pendekatan Multidisiplin”. Yogyakarta: Andi (Anggota Ikapi)

Yunianto Bambang, Lestari Titik, Agus Winarso, 2017 “Aktivitas Antibakteri Salep dengan Bahan Aktif Ekstrak Kunyit, Kencur dan Temu Giring Terhadap Bakteri Staphylococcus Aureus”. Jurnal Kebidanan dan Kesehatan Tradisional, Volume 2, No, 2, September 2017,hlm 60-115

# Zhao F, Yin Y, Lu W, Leong J, Zhang W, Zhang J, Zhang M, Kangde K. 2002. Preparation and histological evaluation of biomimetic three-dimensional hydroxyapatite/chitosan-gelatin network composite scaffolds. Volume 23, Issue 15, August 2002, Pages 3227-3234